Chlorinated Distillation Mass Balance Calculations

NB: Primary reference material produces 0.99 dimensionless quantity of single crystal germanium and hence 0.99 has been used to scale all material input and intermediate products the product system to produce the desired 1 kg single crystal germanium FU of this study.

- Coal combustion power plant, pretreatment and re-volatilization

  - Coal combustion power plant  (Xu et al., 2013)

6500/0.99 = 6566.67 kg lignite coal @ 289 ppm = 1.9 kg Ge content

10 times increase in Ge concentration after combustion of coal results in fly ash quantity required for the same Ge quantity = (6566.67 kg /10) = 656.667 kg fly ash @ 2890 ppm (10 X increased grade) with only 85% Ge recovered in plant = 1.9 kg Ge * 0.85 = 1.61 kg

Mass of fly ash for secondary enrichment = 656.667 kg

  - Materials for briquetting (Borowski, 2021): 10% wt. of fly ash as mass of binder and moisture (water)

Therefore, 65.667 kg each of binder and water are used for briquetting

4:1 binder blend ratio of molasses to slaked lime = 52.5336 kg molasses, 13.1334 kg slaked lime

Mass of material for reburning/revolatilization = fly ash + binder + water = 656.667kg + 65.667kg + 65.667kg = 788.001 kg

  - Energy consumption

Chosen roll presser for the briquetting with feed rate of 5 t/h and 15 kW rating:

Specific Energy = 15 kW /5000 kg/h = 0.003 kWh/kg;

Therefore 788.001 kg material = 788.001 kg × 0.003 kWh/kg = 2.364 kWh

Shaft furnace for re-volatilization consumes 80 kWh/t of waste:

Energy consumed for 788.001 kg material = (1000kg/788.001kg) × 18

0 kWh = 228.426 kWh

Total pre-treatment energy = 228.426 kWh + 2.364 kWh = 230.79 kWh

Germanium-containing coal soot produced from reburning in shaft furnace (100 units are used according to Xu et al. (2013))
100/0.99 = 101.01 kg coal soot recovered from shaft furnace at 16,000 ppm = 1.61 kg Ge content

Waste/gasified material from re-volatilization = 788.001 kg - 101.01 kg = 686.99 kg coal soot

- Acid leaching

351 units of HCl is used to leach 100 units (now 101.01 kg) germanium-containing coal soot to produce 3 units of GeCl4 (Xu et al. (2013))

m(HCl) = 351/0.99 = 354.54 kg, m(GeCl4) = 3/0.99 =3.03 kg

Leaching duration (Rao et al., 2024) = 1 hr; Enamel reactor vessel power rating = 5.5 kW

Energy consumed = 5.5 kW * 1 hr = 5.5 kWh

NB: Actual intermediate product GeCl4 quantity has been adjusted from 3.03 kg (scaled from referenced paper) to 3.24 kg to account for loss (0.01 kg) in distillation purification process and the actual quantity (3.23 kg) needed  to produce next intermediate product GeO2 of mass 1.505 kg from hydrolysis.

- Hydrolysis

GeCl4 + 2H2O = GeO2 + 4HCl

Molecular weights: GeCl4 = 214.4 g/mol; H2O = 18 g/mol and GeO2 = 104.99 g/mol

Given: m(HCl) = 351/0.99 = 354.54 kg; m(GeCl4) = 3/0.99 =3.03 kg = 3030 g

n(GeCl4) = m/Mr = 3030 g / 214.4 g/mol ≈ 14.13 mol

n(GeCl4) = n(GeO2) = ½ n (H2O)

n (H2O) = 2 × 14.13 mol ≈ 28.26 mol; n(GeO2) = 14.13 mol

m = n × Mr

m (H2O) = 28.26 mol × 18 g/mol ≈ 508.68 g = 0.51 kg

m(GeO2) = 14.13 mol × 104.99 g/mol ≈ 1505 g = 1.505 kg (same as 1.49 units used in reference paper which scales to 1.49/0.99 = 1.505 kg)

- HCl Regeneration

From reference material (Adham & Harris, 2014): For 1t feed, process water = 641 kg, Thermal Energy (CH4) = 512 MCal

Total waste acid = coal soot + HCl used – GeCl4 formed + Hydrolysis waste acid + distillation residue

Plant feed (total waste acid) = 101.01 (coal soot) + 354.54 (HCl) – 3.24 (GeCl4) + 11.42  (calculated under hydrolysis section) + 6.235 (check from distillation section)= 469.965 kg

Scaling factor = 469.965 kg/1t = 0.46997

Process water = 641 kg * 0.46997= 301.251 kg

Thermal Energy = 512 MCal * 0.46997= 240.625 MCal

- GeCl₄ purification/distillation

Volume of HCl used = 3 times volume of GeCl₄ (Hoffmann, 1987)

= 3 (mass of GeCl4/density of GeCl4) = 3 (3.24 kg/1.879 g/cm³) = 5,172.96434 cm³ of HCl

Mass of 7M HCl solution = density * volume = 1.09824 kg/L * 5,172.96434 cm³ = 5.68116 kg HCl

Cl2 gas volume (mass) calculation (Ernst & Muro, 1963)

Volume flow rate of Cl₂ gas = 5 L/min Cl2 gas for 0.05 L/min GeCl₄ flow = 100 L Cl₂ per 1 L GeCl₄

Volume (GeCl4) = 3.24 kg/1879 kg/m3 = 0.00172 m³ = 1.72 L GeCl4

1.72 L GeCl4 = (100 L Cl₂/1 L GeCl₄) * 1.72 L GeCl4 = 172 L Cl₂

Using n= V/Vm for ideal gas, n = 172 L/22.4L/mol = 7.6786 mol

Using molar mass of 71g/mol Cl₂, mass of Cl₂= 7.6786 mol * 71g/mol = 0.54518 kg

GeCl4 recovered >> 99% = 3.23 kg GeCl4

Mass of residue = Crude GeCl4 + HCl + Chlorine gas – GeCl4 recovered

Mass of residue = 3.24 kg + 5.68 kg + 0.545 kg – 3.23 kg = 6.235 kg

- Hydrolysis

GeCl₄(l) + 2H₂O (l) → GeO₂(l) + 4HCl(l)

Molecular weights: GeCl4 = 214.4 g/mol; GeO2 = 104.99 g/mol

Given: m(HCl) = m(GeCl4) = 3.23 kg = 3230 g

n(GeCl4) = n(GeO2) = ½ n (H2O) = ¼ n (HCl)

n(GeCl4) = 3230 kg /214.4 g/mol = 15.07 mol = n(GeO2)

m(GeO2) = 104.99 g/mol * 15.07 mol =1582.2 g @ 95% recovery = 1.505 kg GeO2 with 1.04 kg Germanium

Actual usage of deionized water (Hoffmann, 1987) = 3 times the mass of GeCl4

= 3(3.23 kg) = 9.69 kg H₂O

Acid slag (HCl) = m(GeCl4) + m (H2O) - m(GeO2) = 3.23 kg + 9.69 kg – 1.505 kg = 11.42 kg

Energy rating for single-jacketed-glass-reactor component: refrigeration power, circulating pump, hydrolysis reactor motor and stirrer power are 2 kW, 0.28 Kw, 0.37 Kw and 0.2 kW respectively @ Hydrolysis reactor source

Hydrolysis reaction time = 1.5 hrs @ Patent source

Energy consumed = (2 kW+ 0.28 kW + 0.37 kW + 0.2 kW) * 1.5 hr = 4.275 kWh

- Drying/Calcining

Nitrogen gas addition (Gradwohl et al., 2020)

100 L/h for 3 h = 1.7 kg GeO2

1.505 kg = (1.505/1.7) * 100 L/h = 88.529 L/h and (1.505/1.7) * 3 h = 2.6559 h

Volume of N2 used = 88.529 L/h * 2.6559 h = 235.1242 L

Using Molar volume at STP = 22.4 L/mol and Molar mass of N₂ = 28.014 g/mol

Mass = (235.1242 L /22.4 L/mol) * 28.014 g/mol = 294.0522 g = 0.29405 kg N₂

Drying Energy at 120 Celsius (Wang et al., 2014)

Drying Time per kg = 135 min / 0.5 kg = 270 min/kg.

Time for 1.505 kg = 270 min/kg × 1.505 kg = 406.35 minutes (≈ 6.77 hours).

Energy per kg = 1 / 0.09 kg/kWh = 11.11 kWh/kg.

Energy for 1.505 kg = 11.11 kWh/kg × 1.505 kg = 16.72 kWh

95% GeO2 recovered after drying = 0.95 * 1.505 kg = 1.475 kg GeO2

- Reduction

GeO2 + 2H2 = Ge + 2H2O

Actual nitrogen (unreactive) and hydrogen usage (Gradwohl et al., 2020)

1.475 kg GeO2 from drying contains 1.024 kg Ge

Scaling factor = GeO2 quantity/reference GeO2 quantity =1.475 kg/1.4kg = 0.8676

N2 flow rate = 100 L/h * 0.8676 = 86.8 L/h

H2 flow rate = 200 L/h * 0.8676 = 173.5 L/h

Using 8 hours period for reduction in graphite boat (Hoffmann, 1987)

H₂ total volume =173.5 L/h×8 h=1388 L

N₂ total volume =86.8 L/h×8 h=694.4 L

Using n = V/Vm and m = n * M, m = (V/Vm) * M

Where Vm = 22.4 L/mol (molar volume of ideal gas at STP), M (H₂) = 2.016 g/mol and M(N₂) = 28.014 g/mol

Mass of H₂= (1388 L/22.4 L/mol) ×2.016 g/mol = 124.92 g = 0.12492 kg (actual)

Mass of N₂= (694.4L/22.4 L/mol) × 28.014 g/mol = 868.434 g = 0.86843 kg

Residue = GeO2 + Hydrogen gas + Nitrogen gas – Crude germanium = 1.475 kg + 0.125 kg + 0.868 kg – 1.014 kg = 1.454 kg

Compiled LCI Data for Chloride Distillation

| Stage | LCI | Result (per kg of Ge single crystal) | Source/comment |
| --- | --- | --- | --- |
| Pre-treatment & Volatilization | Fly ash Molasses Slaked lime Water Electricity | 656.667kg 52.5336 kg 13.1334 kg 65.667 kg 230.79 kWh |  |
| Acid Leaching | Coal soot HCl Electricity | 101.01 kg 11.11kg 5.5 kWh |  |
| HCl Treatment Plant | Waste acid Thermal energy Process water | 469.965 kg 240.63 MCal 301.25 kg |  |
| Distillation | Crude GeCl₄ Electricity HCl Chlorine gas Residue | 3.24 kg 12.01232 kWh 5.68116 kg 0.54518 kg/172 L 6.235 kg | Intermediate product |
| Hydrolysis | GeCl₄ Deionized water Electricity | 3.23 kg 9.69 kg 4.275 kWh | Intermediate product |
| Drying | GeO2 Electricity Nitrogen gas | 1.505 kg 16.72 kWh 0.29405 kg | Intermediate product |
| Reduction | GeO2 H2(g) N2(g) Electricity Residue | 1.475 kg 0.125 kg 0.868 kg 45.788 KWh 1.454 kg | Intermediate product |
| Zone Refining | Crude Ge metal Electricity Solid waste | 1.04 kg 17.62996 kWh 0.03 kg | Intermediate product |
| Crystal pulling | Ge metal Solid waste Electricity | 1.01 kg 0.004 kg 17.45609 kWh | Intermediate product |

FactSage Thermodynamic Simulation Data Results

| Process Name | Temperature Range (Kelvin) | Simulation result (ΔH°) (J) | kWh Conversion | Factor | Estimated Energy (kWh) |
| --- | --- | --- | --- | --- | --- |
| Fractional Distillation | 298.15 - 356.27 | 619835.8 | 0.172176611 | 69.76744186 | 12.01232171 |
| Reduction & Pre-melting | 298.15 - 1273.15 | 2362652.9 | 0.656292472 | 69.76744186 | 45.7878469 |
| Zone Refining | 298.15 - 1373.15 | 909705.8 | 0.252696056 | 69.76744186 | 17.62995736 |
| Germanium crystal growth (CZ) | 298.15 - 1276.15 | 900734.3 | 0.250203972 | 69.76744186 | 17.45609109 |
| Silicon Crystal Growth | 298.15 - 1700 | 3095391 | 0.859830833 | 69.76744186 | 60 |

Silicon Czochralski crystal growth energy consumed = 60 kWh/kg of single crystal silicon Energy usage source

Factor (F) = (Available Industrial data) / (FactSage Results)

Factor = 60 kWh/0.86 kWh = 69.76744186

Estimated energy = Factor × process simulation energy result

Solvent Extraction Mass Balance Calculations (Arroyo et al., 2009, 2015)

Pilot scale production = 61g/h of aqueous GeO2 produced from fly ash feed rate of 200kg/h and germanium grade of 350 mg/kg

1.505 kg of Aqueous GeO2 obtained from stripping prior to its drying/calcining is the desired intermediate product for subsequent processing to 1 kg single crystal germanium.

Tracing backward from 1.505 kg GeO2 (1.04 kg Ge content) intermediate product in the flowsheet (refer to Appendix Fig. A1 in the manuscript), 1.642 kg Ge content in fly ash is needed based on the Ge recovery at each recovery unit. At 350 mg/kg germanium concentration, 4691.428 kg fly ash is required for the starting 1.642 kg Ge content.

Scaling factor = 4691.428 kg /200kg = 23.45714  (Arroyo et al., 2015) or 4691.428 kg / 5kg = 938.2856 (Arroyo et al., 2009)

NB: We have used Arroyo et al. (2015) with factor 23.45714 for scaling throughout except where desired material/reagent quantity was not repeated in (Arroyo et al., 2015), then, Arroyo et al. (2009) was referred to and scaled with 938.2856.

- Leaching reactor

FA = 4691.428 kg @ 350 mg/kg Ge grade = 1.642 kg Ge content

Scaling factor = 4691.428 kg /200kg = 23.45714

L/S = 5; L (water) = 5 S (fly ash)

Water/liquid requirement = 5(4691.428 kg) = 23457.14 kg = 23457.14 L

75% of liquid requirement provided by raffinate = 0.75 * 23457.14 kg = 17592.855L or kg (assumption that raffinate has same density as water)

Fresh water (25%) = 0.25 * 23457.14 kg = 5864.285 L or kg,

Total mass of mixture (M) in leaching reactor unit = m(FA) + m(Water) = 4691.428 kg + 23457.14 kg = 28148.568   kg = M

Cake (C) produced after leaching has 35% wt. water/liquid

Leachate/water in cake = 104 L* 23.45714 = 2439.542 L = 2439.542 kg representing 35% wt. water/liquid

If 35% of the weight of the cake is water = 2439.542 kg, Total weight of cake representing 100% = (100% / 35%) * 2439.542 kg = 6970.12 kg = m(Cake) = C

- Complexation

Volume of leachate for complexation = 896 L * 23.45714 = 21017.597 L

Mass of leachate for complexation, L = Total Mixture – Cake = M - C = 28148.568 kg - 6970.12 kg = 21178.448 kg

Catechol: If 5 kg/h FA feed rate consumed 16g/h CAT, then, 4691.428 kg FA will consume = 16g * 938.2856 = 15.012 kg = CAT

H2SO4 (10%w) solution: If 5 kg/h consumed 120 mL H2SO4 (10%w), 4691.428 kg will consume = 120 mL * 938.2856 = 112594.272 mL H2SO4 (10%w)

H2SO4 (10%w): Density of solution is approx. 1.0 g/mL, then mass of H2SO4(10%w) = 112594.272 g = 112.594 kg

Mass of H2SO4 in solution = 10% × total mass of solution = 10% × 112.594 kg =11.259 kg

Mass of water = 90% × 112.594 kg = 101.335 kg

- Organic Phase

Kerosene (KER) : If 4.5 L is used for 5kg/h, 4691.428 kg FA = 4.5 L * 938.2856 = 4222.285 L Using density of KER = 0.8 g/mL, mass of KER = 0.8 g/mL * 4222.285 L = 3377.828 kg

95% of required KER is obtained in residual of organic phase (ROP) = 0.95 * 3377.828 kg = 3208.934 kg

Fresh KER needed = 3377.828 kg - 3208.934 kg = 168.894 kg

TOA: If 41mL is used for 5kg/h, 4691.428 kg FA = 41mL * 938.2856 = 38469.71 ml.

Using trioctylamine (TOA) density of 0.809g/mL, m(TOA) = 38469.71 mL * 0.809g/mL = 31.122 kg

95% (29.566 kg) of TOA is obtained in ROP so fresh TOA required= 0.05 * 31.122 kg =1.556kg

Organic phase (OP) mixture = Kerosene + TOA = 3377.828 kg + 31.122 kg = 3408.95 kg

Total ROP reutilized (95% wt) = 3208.934 kg + 29.566 kg = 3238.5 kg

Total fresh OP make-up = 168.894 kg + 1.556 kg = 170.45 kg

- Extraction Mixer

Total mass of Aqueous phase (AP) = L + CAT + H2SO4 (10%w) = 21178.448 kg + 15.012 kg + 112.594 kg = 21306.054 kg

Total mass of organic phase (OP) = KER + TOA = 3377.828 kg + 31.122 kg = 3408.95 kg

Total mixture = AP + OP = 21306.054 kg + 3408.95 kg = 24715.004 kg

- Extraction settler

Total mixture = AP + OP = 21306.054 kg + 3408.95 kg = 24715.004 kg

Raffinate volume = 896 L * 23.45714 = 21017.597 L

If 83.9% of raffinate recovered is reutilized (Arroyo et al., 2015) and represents 75% (17592.855 L or kg) of water/liquid required for solvent extraction, then, total mass of raffinate (100%) = (100% / 83.9%) * 17592.855 kg = 21196.211 kg
Residual raffinate = Total raffinate – reutilized raffinate = 21196.211 kg - 17592.855 kg

Residual raffinate = 3603.356 kg

Organic extract volume = 170.2L * 23.45714 = 3992.405228 L, volume loss = 9.0L * 23.45714 = 211.114L

Organic extract (OE) mass = Total mixture - total raffinate = 24715.004 kg - 20968.838 kg = 3746.166 kg

- Stripping Mixer

Organic extract mass = 3746.166 kg

1 M NaOH solution of 34 L volume; Actual volume =34 L * 23.45714 = 797.543 L

C = n/V, n (NaOH) = Concentration × Volume (in liters)

= 1 M × 797.543 L = 797.543 mol

Mass of NaOH = Number of moles × Molar mass, M (NaOH) = 40 g/mol

= 797.543 mol × 40 g/mol = 31.902 kg

Assuming volume of water ≈ volume of solution = 797.543 L

Mass of water = 797.543 kg

Mass of stripping solution = 31.902 kg + 797.543 kg = 829.445 kg

Total mixture for stripping mixer = Stripping solution + organic extract = 829.445 kg + 3746.166 kg   = 4575.611 kg

- Stripping Settler

Total mixture = Stripping solution + organic extract = 829.445 kg + 3746.166 kg =4575.611kg

Stripping residue/ Residual organic phase = Total mixture – Aqueous extract (as GeO2) - reutilized ROP = 4575.611kg – 1.505 kg - 3238.5 kg = 1335.606 kg

Losses OP = OP – Reutilized ROP = 3408.95 kg - 3238.5 kg = 170.45 kg

Energy/Power Requirement (Arroyo et al., 2015)

- Leaching reactor unit

2.7 m³ leaching reactor

Required power = 0.5 kW

Residence time: 2 hrs per process * 23.45714 = 46.91 hrs

Electrical power consumption = 0.5 kW * 46.91 hrs = 23.455 kWh (A)

- Filtering

2 filter pressers with filtering area of 5.6 m²

The designed filtering plate is 500 mm with 23 plates required.

0.3 - 3.3 kW at 2 hours per filtration cycle for 1792 L

Hence 28148.568 kg of fly ash- water mixture approximated to be 28148.568 L = 28148.568 L / 1792 L = 16 filtration cycles

Using 3 kW @ 2hrs per cycle * 16 cycles = 96 kWh (B)

- 5 stage Extraction Mixer-settler Cascade

Required Power = 0.02 kW

Extraction time= 5 minutes * 23.45714 = 1.955 hrs

Electricity consumption = 0.02 kW * 1.955 hrs = 0.0391 kWh (C)

- 9 Stage Stripping Mixer-settler Cascade

Required Power = 0.02 kW

Stripping time = 5 minutes * 23.45714 = 1.955 hrs

Electricity consumption = 0.02 kW * 1.955 hrs = 0.0391 kWh (D)

Total SX process energy requirement = A + B + C + D = 23.455 kWh + 96 kWh + 0.0391 kWh + 0.0391 kWh = 119.5332 kWh

LCI for Solvent Extraction

| Stage | LCI | Result (per kg of Ge single crystal) | Source/comment |
| --- | --- | --- | --- |
| Leaching | Fly Ash Water Reutilized raffinate Electricity Cake (35% water) | 4691.43 kg 5,864.28kg 17,592.855 kg 23.455 kWh 6,970.12 kg | Avoided landfill |
| Complexation | Leachate Catechol H₂SO₄ Water | 21,178.45kg 15.01kg 11.26 kg 101.34 kg | Intermediate product |
| Extraction | Extraction mixture Kerosene Trioctylamine Total Raffinate Raffinate residue | 24,715 kg 168.89 kg 1.556 kg 21,196.211 kg 3,603.36 kg | Intermediate product |
| Stripping | Stripping mixture NaOH Water Stripped phase raffinate | 4575.611 kg 31.90 kg 797.54 kg 1,335.61 kg | Intermediate product |
| Drying | GeO2 Electricity Nitrogen gas | 1.505 kg 16.72 kWh 0.29405 kg | Intermediate product |
| Reduction | GeO2 H2(g) N2(g) Electricity Residue | 1.475 kg 0.125 kg 0.868 kg 45.788 KWh 1.454 kg | Intermediate product |
| Zone Refining | Crude Ge metal Electricity Solid waste | 1.04 kg 17.62996 kWh 0.03 kg | Intermediate product |
| Crystal pulling | Ge metal Solid waste Electricity | 1.01 kg 0.004 kg 17.45609 kWh | Intermediate product |

References

Adham, K., & Harris, C. (2014). HCL ACID REGENERATION FOR CHLORIDE BASED HYDROMETALLURGICAL PROCESSES WITH MINIMUM ENVIRONMENTAL IMPACT HYDROMETALLURGY 2014-VOLUME II HCL ACID REGENERATION FOR CHLORIDE BASED HYDROMETALLURGICAL PROCESSES WITH MINIMUM ENVIRONMENTAL IMPАСТ PROCEÉDINGS OF THE 7TH INTERNATIONAL SYMPOSIUM. https://www.researchgate.net/publication/331022331

Arroyo, F., Fernández-Pereira, C., & Bermejo, P. (2015). Demonstration plant equipment design and scale-up from pilot plant of a leaching and solvent extraction process. Minerals, 5(2), 298–313. https://doi.org/10.3390/min5020298

Arroyo, F., Fernández-Pereira, C., Olivares, J., & Coca, P. (2009). Hydrometallurgical recovery of germanium from coal gasification fly ash: Pilot plant scale evaluation. Industrial and Engineering Chemistry Research, 48(7), 3573–3579. https://doi.org/10.1021/ie800730h

Borowski, G. (2021). USING OF ADHESIVES AND BINDERS FOR WASTE AGGLOMERATION. https://doi.org/https://www.sardiniasymposium.it/public/documents/poster-files-2021/p01_paper_borowski.pdf

Ernst, R. G., & Muro, L. V. (1963). Purification of Germanium Tetrachloride.

Gradwohl, K. P., Moras, O., Janicskó-Csáthy, J., Schönert, S., & Sumathi, R. R. (2020). Hydrogen reduction of enriched germanium dioxide and zone-refining for the LEGEND experiment. Journal of Instrumentation, 15(12). https://doi.org/10.1088/1748-0221/15/12/P12010

Hoffmann, J. E. (1987). Extracting and Refining Germanium. JOURNAL OF METAL, 39, 42–45. https://doi.org/https://doi.org/10.1007/BF03258062

Rao, M., Xu, Y., Xia, H., Jiang, G., Dai, L., & Zhang, L. (2024). Hydrochloric Acid Leaching Kinetics Study of Germanium Concentrate. JOM, 76(12), 7209–7217. https://doi.org/10.1007/s11837-024-06895-7

Wang, S. L., Liu, Y. Bin, Zhang, D. Bin, Peng, M. Q., & Wang, R. S. (2014). Research and application of new drying process for germanium dioxide. Advanced Materials Research, 997, 101–105. https://doi.org/10.4028/www.scientific.net/AMR.997.101

Xu, D., Chen, Y. W., Guo, H., Liu, H. Q., Xue, Y. D., Zhang, W. F., & Sun, Y. C. (2013). Review of Germanium recovery technologies from coal. Applied Mechanics and Materials, 423–426, 565–573. https://doi.org/10.4028/www.scientific.net/AMM.423-426.565